## Slide 1: Processing of Electroactive Components by means of Selective Laser Sintering / Melting (SLS/SLM)
Fifteenth European Inter-Regional Conference on Ceramics
CIEC 15 5th-7th September 2016
M. Gonon, N. Basile

## Slide 2: Context
Ceramic materials are the functional materials of a large number of electronic components.
Complexes devices are composed of superimposed layers (conductors, semi-conductors, dielectrics, …) directly bounded over an insulating substrate.
Processing such devices requires numerous deposition / firing steps :
Time and energy consumption
Firing conditions must be compatible with thermal stability of all already deposited materials.
Compromises in terms of compositions and final microstructure and properties
conductors
Functional layer
Substrate
Substrate cleaning
Ink serigraphy
Drying
Firing
Final component
x n

## Slide 3: Context
Laser source
Machining
Welding / brazing
Cladding alloying
Surface treatment (quenching , vitrification ; crystallization)
Additive manufacturing

## Slide 4: Context
Would it be possible to consolidate and densify the different layers of an electronic component by mean of a laser beam ?
Lasesurf projet
Conductive metallic tracks
Electroactive ceramics layers

## Slide 5: Selective laser melting / sintering
0 Dimension
dots
1 Dimension
lines
2 Dimensions
areas
static
static
dynamic
Laser treatments

## Slide 6: Selective laser melting / sintering
Temperature (°C)
Relative density
Specific surface (m²/g)
Sintering
Time
Porosity
Relative density
Intermediate stage
Initial stage
Final stage
Mechanisms
Grains bridging
Densification
Grain growth
Phases transformation
Time
Temperature
Parameters
Sintering of a powder layer
mismatch layer / substrate
Shrinkage (Porosity resorption)
Temperature gradients
Thermal expansion

## Slide 7: Selective laser melting / sintering
Sintering of a powder layer
Temperature of the grains
    → true power density (absorbed)
    → grains size, shape, specific energy and thermal conductivity
    → interaction time
Interaction time
    → dynamic or stationary
    Dynamic mode = Short interaction time
    → non stationary regime + complex thermal history
    → thermal gradient between surface and center of the grains.
    → compatibility with diffusion kinetics ?
    → Fast local heating and cooling = thermal chocks

## Slide 8: Selective laser melting / sintering
Power density (W/mm2) : Pw = P / (pφ2/4)
Interaction time (s) : t* = ts x (Sbeam / Sscan) = p φ2/ (4 v s)
Energy density (J/mm²) : J* = Pw t* = P / (s v)
Overlapping (%) : Ov = 100 (f – v) / f
Power P (W)
Speed s (mm/s)
Vectorization
v (µm)
Beam diameter
f (µm)
Processing parameters
Scan strategy
1 way or 2ways

## Slide 9: Selective laser melting / sintering
Laser Cladding: Jan Gedopt, Marleen Rombouts Lasercentrum Vlaanderen
Processing parameters
Interaction time (s)
Sintering ?

## Slide 10: Selective laser melting / sintering
Example of the use of a laser beam as energy source to built up layer by layer a complex 3D monolithic structure (additive manufacturing).
Processing parameters
Thermal history

## Slide 11: Lasesurf Projet
Application to thick powder layers deposited on a substrate ?
Problems :
Very short time of treatment
Already dense substrate
Multi materials
Selected material : BaTiO3
Objective : process a 10 to 100 µm tick layer on an alumina substrate
Challenge

## Slide 12: Lasesurf Projet
Procedure
1 : Treatment of BaTiO3 powder pellets.
Parameters leading to a consolidation of the surface
Characterize the microstructure
Identify consolidation mechanisms
2 : Treatment of a BaTiO3 powder layer
Powder deposited on an alumina substrate Ag coated or not.
Influence on the scanning conditions
BaTiO3
BaTiO3
Alumina
Ag
BaTiO3
Alumina

## Slide 13: Treatment of BaTiO3 powder pellets
Trumark Station 5000 (Trumpf)
Solid-state laser (Nd-YVO4)
Pmax = 22,8 W (cw)
l = 1064 nm
f = 45 µm
s = 0 to 7000 mm/s
Characterization :
Visual aspect
XRD
SEM
Equipment / Characterization

## Slide 14: Treatment of BaTiO3 powder pellets
BaTiO3 pellets
Parametric investigation
Tetragonal BaTiO3 Powders :
micro, d50 = 0,44 µm (Sigma Aldrich)
nano, d50 = 50 nm (Inframat Advanced Materials )
mixtures micro / nano
Scanned area
10 x 10 mm2
Pw = P / (pφ2/4)
t* = p φ2/ (4 v s)
J* = Pw.t*

## Slide 15: Treatment of BaTiO3 powder pellets
Influence of scan parameters
Influence of s and v
P = 100 % (22,8 W)
Pw = 1,4 106 W/cm2
s = 80 mm/s
v = 10 µm
t* = 2 ms
J* = 2,85 kJ/cm2
s = 1000 mm/s
v = 10 µm
t* = 0,16 ms
J* = 0,228 kJ/cm2
Pw = P / (pφ2/4)
t* = p φ2/ (4 v s)
J* = Pw.t*
15 % nano

## Slide 16: Treatment of BaTiO3 powder pellets
Influence of s and v
t* = p φ2/ (4 v s)
same s.v = same t* and then same J*
High temperature forms of BaTiO3 if t* > 0,13 ms
Amorphous phase if t* > 0,04 ms
But differences in t* limits according to v and s

## Slide 17: Treatment of BaTiO3 powder pellets
For given Pw and t*, the thermal profile of a given point of the scanned surface will be depending on it distance to the laser beam vs time.
If speed is lowered and vectorisation increased, the laps of time between two close positions increases what favor cooling before reheating.
v1, s1
2v1, s1/2
Influence of s and v
t* = p φ2/ (4 v s)

## Slide 18: Treatment of BaTiO3 powder pellets
High amount of glassy phase.
→ Melting of nano and significant part of micro grains.
High temperature crystal form of BaTiO3.
→ high rise in temperature of the core of the larger grains.
Influence of s and v

## Slide 19: Treatment of BaTiO3 powder pellets
Low amount of glass phase.
→ Melting of nano grains ?
Low temperature crystal form of BaTiO3 and weak grain growth of the unmelted grains.
→ limited elevation of temperature of the core of the larger grains.
Influence of s and v

## Slide 20: Treatment of BaTiO3 powder pellets
s < 200 mm/s → glassy surface.
→ melting of a large part of the grains.
→ phase transformation and growth of unmelted grains.
Comparison mix micro + nano / pure micro
weak cohesion of sanned surfaces for s > 200 mm/s
Influence of s and v

## Slide 21: Treatment of BaTiO3 powder pellets
Higher t* limits if Pw decreases from 100 % down 95% and 90%.
However, no cohesion of scanned surface if P < 90 % (Pw = 1,3 106 W/cm2).
→ the increase in t* thorough a decrease in s doesn't compensate the decreased in Pw (a cte J* is not sufficient to lead to a same result).
Influence of P and s
v = 10 µm
Pw = P / (pφ2/4)
t* = p φ2/ (4 v s)
J* = Pw.t*

## Slide 22: Treatment of BaTiO3 powder pellets
Conclusion influence of scan parameters
Possible to obtain consolidated t-BaTiO3 layers.
Need of a fraction of fine grains that melt for “low” energetic conditions.
Interaction time t* must be short enough to limit the melted fraction and avoid phase transformation of the larger grains.
  t* limit depend on vectorisation v and speed s.
Energy density J* is not a pertinent parameter : Pw cannot be lowered below 1,3 106 W/cm2.

## Slide 23: Consolidation of a BaTiO3 powder layer
Procedure
1 : Treatment of BaTiO3 powder pellets.
Parameters leading to a consolidation of the surface.
Characterize the microstructure.
Identify consolidation mechanisms.
2 : Treatment of a BaTiO3 powder layer
Powder deposited on an alumina substrate Ag coated or not.
Influence on the scanning conditions.
BaTiO3
BaTiO3
Alumina
Ag
BaTiO3
Alumina

## Slide 24: Treatment of BaTiO3 powder layers
Interaction during a line scan
25 µm BaTiO3 layers
80 µm
P = 100 % ; s = 1.000 mm/s

## Slide 25: Treatment of BaTiO3 powder layers
Interaction during a line scan
80 µm
P = 100 % ; s = 1.000 mm/s
80 µm
20 µm
Pellets
Substrate

## Slide 26: Treatment of BaTiO3 powder layers
Surface scan
BaTiO3 layer on alumina substrate
P = 100 % ; s = 1.000 mm/s ; v = 40 µm
P = 100 % ; s = 2.000 mm/s ; v = 20 µm
P = 100 % ; s = 4.000 mm/s ; v = 10 µm
t* = p φ2/ (4 v s)
40 µs

## Slide 27: Treatment of BaTiO3 powder layers
Conclusion powder layers
Problem of interaction with the substrate.
High temperatures reach by the powder layer not compatible with low temperature melting conductors as Ag.
Thermal gradients between the layer and the substrate cause dilatation / shrinkage mismatches generating stresses and cracks.
Target :
more homogeneous heating.
Avoiding melting (real solid state sintering).
Thermal characterization of the scanned surface during the laser treatment

## Slide 28: Thermal characterization of a laser scan
Infrared camera : FLIR AGEMA 750 PAL objectif FOV 24,
acquisition time : 2 s
Scanned Surface : 10 x 10 mm2
Spatial resolution : 12 x 8 mm2
Number of cells : 96 (8 x 12)

## Slide 29: Thermal characterization of a laser scan
Vectorisation
Power density : 1,4 106 W/cm2
Vectorisation : 40 µm
Scan speed : s = 10 mm/s
Interaction time : t* = 3,5 10-3 s
20s

## Slide 30: Thermal characterization of a laser scan
Vectorisation
Power density : 1,4 106 W/cm2
Vectorisation : 40 µm
Scan speed : s = 10 mm/s
Interaction time : t* = 3,5 10-3 s

## Slide 31: Thermal characterization of a laser scan
t* = p φ2/ (4 v s)
Vectorisation
Scan speed : s = 30 ; 10 ; 5 mm/s

## Slide 32: Thermal characterization of a laser scan
Vectorisation
t* = p φ2/ (4 v s)
10 x 10 mm2
10 x 20 mm2
20 x 10 mm2
Scan speed : s = 10 mm/s

## Slide 33: Thermal characterization of a laser scan
At high speed, time resolution of IR camera (2 s) doesn't allow to follow temperature of a selected zone during 1 cycle.
Repeated cycles :
Min ; Average and Max temperature of the scanned surface vs time.
Influence of speed.
1000 mm/s
5000 mm/s

## Slide 34: Thermal characterization of a laser scan
1000 mm/s
5000 mm/s
Weak heating of the cells during the first cycles.
Heating is limited to a little area around the laser beam.
High temperature gradient over the scanned surface a low speed.
Limited gradient at high speed.

## Slide 35: Thermal characterization of a laser scan
A temperature plateau is reached after 80 s.
The maximum temperature is not influenced by the speed.
The heating rate at sort time is higher for high speeds.

## Slide 36: Thermal characterization of a laser scan
Conclusion thermal characterization
Interaction time t* is not a characteristic parameter.
short vectorisation v and high speed s = more progressive and homogeneous heating.
Possibility of increasing interaction time by mean of a multiscan strategy.
= very short interaction time during one cycle (very high speed) but repeated several times.
= control of the heating profile of the scanned surface.
t* = p φ2/ (4 v s)

## Slide 37: Thermal characterization of a laser scan
Conclusion thermal characterization
100 µm BaTiO3 Layer
P = 100 % ; v = 40 µm
Consolidation but no densification
s = 5.000 mm/s ;
s = 2500 mm/s ;
X 60 s

## Slide 38: Thermal characterization of a laser scan
Conclusion / outlooks
Possibility to consolidate and densify a BaTiO3 layer through the melting of a low volume fraction of small powder grain.
But not compatible with other materials.
Mismatch with the substrate leading to cracks.
A real solid state sintering requires an increase of the total time of treatment while keeping a homogenous controlled heating of the surface :
= Mutiscan strategy
The maximum temperature reached in the stationary regime do not depend on the scanning speed but on the power density of the laser beam.
Limit of the equipment

## Slide 39
  Thank you for your attention