## Slide 1: Efficiency and durability of a bioactive coating in formaldehyde degradation
18 September 2019
Cristiana C. Castro, Tangi Senechal, Julian Viseur,
Ducoulembier Aline, Driss Lahem, Anne-Lise Hantson

## Slide 2: Problem
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
Indoor air pollution
Health and comfort concerns
Main contaminants
  Mold and bacteria
  Dust and other allergens
  Gases (NO, CO and CO2)
  Chemicals and solvents
VOCs: Volatile organic compunds
VOCs
Legislation limits

## Slide 3: Formaldehyde
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
Exposure time
Concentration
FA
Eyes, nose and throat irritation
Breathing difficulties
Respiratory injuries
Chronic pulmonary obstruction
Pulmonary cancer
Immunogenic
Mutagenic
Allergenic
Carcinogenic
Construction materials
Wood processing
Furniture
Textiles
Carpeting
Cleaning products
> 0.3 ppm
≈ 4 h

## Slide 4: Technology and Innovation
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
Surface
Odors
VOCs
Mold
Bacteria
Gases
H2O
O2
CO2
N2
…
Technology
Innovation
Capture and degradation of contaminants by encapsulated microorganisms and/or biomolecules
Placement of the wet coating on structural elements (ventilation ducts, ceiling tales, glazed areas)
Environmental and health friendly technology
Durable and rechargeable

## Slide 5: BIODEC Solution
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
Furniture
Paints
Cosmetics
Smoking
Odors VOCs
Bacteria
Gases Mold
Bioactive Coating
Cleaning products
H2O
O2
CO2
N2
…
Indoor DEpollution
Encapsulation:
Bioactive
molecules
Microorganisms
with depolluting
ability

## Slide 6: FA-degrading strains
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS

## Slide 7: FA-degrading enzymes
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
Catabolic pathways
Anabolic pathways

## Slide 8: Coatings formulation
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
sol-gel coating
  Mechanical properties
  Control of the hydrophobicity
  Chemical resistance
  Durability
Enzymes viability
  Low temperature
  No alcohol
  No extreme pH
  No UV
  No Ultrasound
TEOS
GPTMS
PVOH
PEG
With water and acetic acid
sol-gel coating - precursors

## Slide 9: Microorganisms preparation
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
Pseudomonas putida
No biological activity
Active enzymes
Water dispersible
Bioreactor production
Freeze drying
Dried cells

## Slide 10: Coatings preparation
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
Incorporation of freeze-dried
Pseudomonas putida
Solution
of precursors
Condensation
Sol-gel
Spray
Coated substrate
(Thin-layer chromatography (TLC) paper)
Dense thin film

## Slide 11: Experimental design – coatings formulation
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
Optimised experimental design (OED)
  3 variables: Sol-gel; PEG; [microorganism]
  2 levels
Responses:
  Max. FA degradation
Coatings were applied on the surface of the TLC paper according to OED
Coating deposition by spray
Number of application layers = 6
Reactional mixture (4 mL):
8 pieces of papier CCM (1 cm2)
1 mM Formaldehyde
1 mM NAD+
Carbonate buffer, pH = 10

## Slide 12: FA degradation at room temperature (+/- 20°C)
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
Chart: Time (h)
| 0 | 17.75 | 23.830000000000005 | 48
Série 1 | 2.983 | 0.347 | 0.519 | 0.339
Série 2 | 2.96 | 2.001 | 1.695 | 0.451
Série 3 | 2.91 | 2.498 | 2.432 | 1.871
Série 4 | 2.918 | 2.733 | 2.612 | 2.536
Série 5 | 2.909 | 2.525 | 2.204 | 1.543
Série 6 | 3.081 | 2.594 | 2.459 | 2.117
Série 7 | 2.871 | 0.853 | 0.619 | 0.439
Série 8 | 2.921 | 1.697 | 1.258 | 0.255
Optimal conditions: series 1 and 7
FA degradation yield is kept during 5 weeks for series 1 (~ 90%) and 7 (~ 77%)
Decrease of degradation yield for series 2 et 8
The presence of PEG in serie 1 allowed the retention of large contents of water that improved the activity of formaldehyde-degrading enzymes
Chart: Time (h)
| 0 | 5.17 | 22.330000000000005 | 28.8 | 46.36
Série 1 | 2.973 | 1.997 | 0.559 | 0.508 | 0.441
Série 2 | 2.934 | 2.376 | 1.993 | 1.902 | 1.568
Série 3 | 2.876 | 2.908 | 2.966 | 2.911 | 2.648
Série 4 | 2.967 | 2.798 | 2.705 | 2.87 | 2.258
Série 5 | 3.017 | 2.632 | 2.213 | 2.558 | 2.369
Série 6 | 2.965 | 2.638 | 2.542 | 2.567 | 2.256
Série 7 | 2.977 | 2.36 | 1.635 | 1.462 | 0.806
Série 8 | 2.886 | 2.467 | 2.092 | 1.974 | 1.73
24h after deposition
5 weeks after deposition

## Slide 13: Coatings durability
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
Deposition on TLC surface

## Slide 14: Conclusions
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
Bioactive coatings containing freeze-dried bacterial cells were efficient in formaldehyde degradation in solution
The presence of PEG in the sol-gel improves the enzymatic degradation of the pollutant
Coatings storage at 37°C decreased formaldehyde degradation ability
Formaldehyde degradation efficiency can be kept by storing sol-gel coatings at room temperature
Further studies should be carried out to study the conservation of enzymes stability throughout time for industrial application of the bioactive coatings

## Slide 15: Aknowledgments
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
BIODEC collaborators
GPCB team

## Slide 16
HANTSON Anne-Lise| Applied Chemistry and Biochemistry Department, Faculty of Engineering, UMONS
Questions?